Table 1. Fertilizer formulations dried by Spray Drying.

| Carrier /AI Ratio | Chitosan 1% w/v Solution (mL) | Potassium Phosphate 1% w/v Solution (mL) | Milli-Q Water (mL) | Final Volume (mL) |
| --- | --- | --- | --- | --- |
| 5/2 | 25 | 10 | 65 | 100 |
| 1/1 | 25 | 25 | 50 | 100 |
| 5/1 | 25 | 5 | 30 | 100 |
| 1/2 | 25 | 50 | 25 | 100 |

Table 2. Levels for the experimental variables.

| Factor | Experimental Domain |  |
| --- | --- | --- |
|  | Level (-) | Level (+) |
| Temperature | 120 °C | 150 °C |
| Air Pressure | 0.2 MPa | 0.4 MPa |
| Feed Rate | 1.4 mL/min | 3.6 mL/min |
| Extraction Rate | 6 m³/min | 10 m³/min |

Table 3. Particle size measured for each iteration.

| Iteration | Temperature (°C) | Air Pressure (MPa) | Extraction Rate (m³/min) | Feed Rate (mL/min) | Particle Size (µm) |
| --- | --- | --- | --- | --- | --- |
| 1 | 120 | 0.2 | 6 | 1.4 | 1.3621 |
| 2 | 150 | 0.2 | 6 | 1.4 | 1.8102* |
| 3 | 120 | 0.4 | 6 | 1.4 | 1.4506 |
| 4 | 150 | 0.4 | 6 | 1.4 | 1.3068* |
| 5 | 120 | 0.2 | 10 | 1.4 | 1.0823* |
| 6 | 150 | 0.2 | 10 | 1.4 | 1.1847 |
| 7 | 120 | 0.4 | 10 | 1.4 | 1.5409 |
| 8 | 150 | 0.4 | 10 | 1.4 | 1.3471 |
| 9 | 120 | 0.2 | 6 | 3.6 | 1.2971 |
| 10 | 150 | 0.2 | 6 | 3.6 | 1.5510 |
| 11 | 120 | 0.4 | 6 | 3.6 | 1.8754 |
| 12 | 150 | 0.4 | 6 | 3.6 | 1.8842 |
| 13 | 120 | 0.2 | 10 | 3.6 | 2.0447* |
| 14 | 150 | 0.2 | 10 | 3.6 | 1.3361 |
| 15 | 120 | 0.4 | 10 | 3.6 | 1.4575 |
| 16 | 150 | 0.4 | 10 | 3.6 | 1.5057* |

*Treatments chosen for the phosphate release experiments.

Table 4. Encapsulation efficiency for the systems tested.

| Particle Size ( µm) | Encapsulation Efficiency |
| --- | --- |
| 1.0823 | 88.38 % |
| 1.3068 | 90.29 % |
| 1.5057 | 89.37 % |
| 1.8102 | 91.08 % |
| 2.0447 | 92.67 % |