Dear Prof. Ignacio González-Martínez

Hi

We wish to submit an original research article entitled “Recyclable Nanomagnetic Fe3O4@APTES catalyst role on the Hydrolysis of Polycarbonate Wastes” as the full article for publication in Journal of the Mexican Chemical Society.

I would like to disclose the following information about the project: I am the corresponding author of this study and contributions of the authors with their responsibility in the research are as follows: Samira Emami and Mir Mohammad Alavi Nikje*.

We confirm that this manuscript does not have plagiarism and has not been published elsewhere; is currently not being considered for publication by any other journal and will not be submitted for such a review while under review by the Journal; the manuscript contains no libellous or other unlawful statements and does not contain any materials that violate any personal or proprietary rights of any other person or entity. All author have approved the manuscript and agree with its submission to Journal of the Mexican Chemical Society.

In this paper, the effect of (3-Aminopropyl) triethoxysilane (APTES) modified Fe3O4  (Fe3O4@APTES) core-shell nanomaterials as the recyclable heterocatalyst on the recovery of bisphenol-A (BPA) from Polycarbonate (PC) wastes were investigated. In the evaluated reactions, water and diethylene glycol (DEG) were used as the green solvent composition and the water as well as magnetic heterocatalyst content were optimized. This is significant because, PC as the useful engineering thermoplastic due to its unique properties is widely used in various applications. Because of unprecedented increase in PC wastes recycling expansion in recent years with features such as low cost, eco-friendly, and easy has become necessary. By examining the results of the above-mentioned reactions, it was observed that by using 25 pbw of water and 2 pbw magnetic heterocatalyst (both based on total waste and solvent weights), pure BPA achieved in 100% yield. The Fe3O4@APTES nanomaterials as the heterocatalyst can be recovered and reused up to five intervals with our significant activity losses. In this way, we have managed to recover the catalyst as one the main goal of green chemistry. The resulting BPA and nanomaterials has been characterized by thermogravimetric analysis (TGA), X-ray diffraction (XRD), and spectroscopic methods (1H NMR, 13C NMR, FT-IR). We believe that this manuscript is appropriate for publication by Journal of the Mexican Chemical Society because it, in this research is shown that PC wastes was recycled using hydrolysis method with features such as inexpensive, convenient, safe, eco-friendly, simple and easy to recovering of pure BPA with high yields 100%. All reactions were performed using water and DEG as the main solvent and co-solvent respectively, effective amount of Fe3O4@APTES as nano-magnetic heterocatalyst at atmospheric pressure.

It should be noted that Microsoft Office Word 2013 was used to write the article.

If you feel that the manuscript is appropriate for your journal, we suggest the following reviewers:

- Feng Xue, College of Material Science and Engineering, South China University of Technology, Guangzhou 510640, China, (psfxue@scut.edu.cn).

- Nayeleh Deirram, Faculty of Chemical Science, Universiti Teknologi Malaysia (UTM), johour 81200, Malaysia, (n.deyrram@gmail.com).

- Huang Jie, Research Institute of Chemical Technology, East China University of Science and Technology, 130 Meilong Road, Shanghai 200237, PR China, (jieh@ecust.edu.cn).

- Deepak Pant, Department of Environmental Sciences, Central University of Himachal Pradesh, Dharamshala, Himachal Pradesh – 176215, India, (deepakpant1@rediffmail.com).

- Zhiyan Pan, Department of Environmental Engineering, Zhejiang University of Technology, Chaowang Road, Hangzhou 310032, China, (panzhiyan@zjut.edu.cn).

- Yasuhiko Kondo, Institute for Energy Technology, National Institute of Advanced Industrial Science and Technology, Tsukuba west, 16-1 Onogawa, Tsukuba-shi, Ibaraki-ken 305-8569, Japan, (y.kondou@aist.go.jp).

- Hiroshi Inomata, Research Center of Supercritical Fluid Technology, Tohoku University, 6-6-11 Aoba, Aramaki, Aoba-ku, Sendai 980-8579 Japan, (inomata@scf.che.tohoku.ac.jp).

Please address all correspondence concerning this manuscript to me at:

Department of Chemistry, Faculty of Science, Imam Khomeini International University, P.O. Box 288, Qazvin, Iran, Telephone number: +98(28)33901268, Fax number: +98(28)33780040, [Email: Drmm.alavi@gmail.com].

Thank you for receiving our manuscript and considering it for review. We appreciate your time and look forward to your response.

Best regards,

Prof. Mir Mohammad Alavi Nikje